## Slide 1: Interatomic potentials for oxide glasses
Warisa Roongaraya
Yiyang Zhu
Andres Ramos

## Slide 2: Available interatomic models with charges:
Rigid ionic models:
  Born-Mayer-Huggins (BMH)
  TTAM Tsuneyuki
  Pedone Potential (PMMCS)
Polarizable interatomic models :
  BMP-FF
  Polarizable Ionic Model (PIM)
Reactive Force-Fields:
  ReaxFF model

## Slide 3: Characteristics of Rigid Ionic Models:
Ions are treated as fixed in space.
Assume spherically symmetric electronic charge distribution.
Ions interact through Coulomb potential.
Commonly used to describe ionic solids.

## Slide 4: Born-Mayer-Huggins (1976 - 1985)
Functional form:
Potential based on long-rage Coulomb term and short-range term (repulsion).
Charge type: formal
N-Body: 2
Simulation results:
  High amount of over-coordinated silicon ions.
  Irregular tetrahedral geometry of units.
  No boroxol rings for borates and borosilicate glasses.

## Slide 5: TTAM - Tsuneyuki
Functional form:
Potential based on Coulomb pair potential and Buckingham potential.
Charge type: partial
N-Body: 2
Simulation results:
  Partial charges lead to better representation of intertetrahedral angle for O-Si-O
  Overestimation of angle due to lack of polarization.
  Represent accurately structure and several thermo-mechanical properties of various silica polymorphs and silica glass.

## Slide 6: Pedone Potential (PMMCS)
Functional form:
Potential based on Coulomb pair potential, Morse potential and repulsive contribution of
Charge type: partial
N-Body: 2
Simulation results:
  Predict mechanical properties accurately
  .
  .

## Slide 7: Available interatomic models with charges:
Rigid ionic models:
  Born-Mayer-Huggins (BMH)
  TTAM Tsuneyuki
  Pedone Potential (PMMCS)
Polarizable interatomic models:
  BMP-FF
  Polarizable Ionic Model (PIM)
Reactive Force-Fields:
  ReaxFF model

## Slide 8: Bertani-Menziani-Pedone (BMP-FF)
Functional form:
Additional terms:
Potential based on Pedone plus three modifications:
  Three-body Interactions described by harmonic functional forms.
  Repulsive interactions.
  Refining pair-wise parameters using DFT reference data.
Charge type: partial
N-Body: 3
Simulation results:
  Better reproduction of density, structure and mechanical properties than original Pedone model.
  .
  .

## Slide 9: Polarizable Ionic Model (PIM)
Functional form: https://link.springer.com/article/10.1007/s00214-012-1143-9
Potential based on four components:
  Charge-Charge
  Dispersion
  Overlap repulsion
  Polarization
Charge Type: formal
N-Body: 3
Characteristics / Simulation results:
  Not widely applied due to complexity and lack of transferability.

## Slide 10: Available interatomic models with charges:
Rigid ionic models:
  Born-Mayer-Huggins (BMH)
  TTAM Tsuneyuki
  Pedone Potential (PMMCS)
Polarizable interatomic models:
  BMP-FF
  Polarizable Ionic Model (PIM)
Reactive Force-Fields:
  ReaxFF model

## Slide 11: Reactive Force Fields

## Slide 12: Models available on LAMMPS

## Slide 13: Table comparing available models on LAMMPS

## Slide 14: Conclusions

## Slide 15
Thank you for your attention.